## Slide 1: Update on R1-A: Quantitative 3-D Analysis of the Canal Network in Pediatric OI Bone
John Jameson (OREC Fellow, UC Berkeley)
RERC Annual Meeting, RIC, Chicago, IL
11/13/2012
Notes: -15 minutes for presentation & questions

## Slide 2: Why Study Bone Structure?...or, What Makes a Bone Strong?
Microstructure
-Bone material
-Vasculature
Mineralization
-Bone Mineral Density
-Bone Mineral Content
Mechanical Loading
-Gait Analysis
-Muscle Forces
Mechanical Properties
-Strength
-Toughness
Notes: -My interests lie at the intersection between gait analysis, microstructural analysis, and mechanical properties

## Slide 3: Why Study Bone Structure?
Rat bone:
  Matsumoto 2005 & 2007: Disuse causes decrease in porosity and connectivity without corresponding decrease in BMD
Human bone:
  Chen 2010: Cortical porosity and canal diameter increase with advanced aging
  Barth 1992: Cortical porosity and canal diameter higher in women with hip fracture
  Snyder 1992: Bone density only moderately correlated with strength!
Healthy
Disuse
62-yo male
92-yo male
Matsumoto et al 2007
Chen et al 2010
Notes: 1:5-10K worldwide, 25-50K US
Limb deformity, short stature, respiratory problems, hearing loss…
Type 1 most common (~50%), but least severe

## Slide 4: Osteogenesis imperfecta (OI)
Mechanical Loading
  Graf 2009: Increased double support, decreased ankle ROM and push-off power
Mechanical Properties
  Fan 2007, Albert 2012: Increased modulus
Bone Mineralization & Microstructure
  Boyde 1999: Increased mineralization density for all OI Types compared to controls
  Rauch 2000: Decreased cortical thickness (Ct.Th)
C
I
III
IV
Albert et al 2012
Rauch et al 2000
Ct.Th
Notes: 1:5-10K worldwide, 25-50K US
Limb deformity, short stature, respiratory problems, hearing loss…
Type 1 most common (~50%), but least severe

## Slide 5: Cortical bone hierarchical structure
Solid material
Cortical bone
(>3000 µm)
Osteons
Lamellae + vasculature
(100-300 µm)
Collagen
Mineralized triple helices
(<1 µm)
Fibrils
Staggered
bundles of
molecules
(~1 µm)
Fiber arrays
“Plies” at different
orientations
(~5-20 µm)
Whole bone
Femur
Notes: -Understanding how OI affects bone at the many different levels allows us to investigate different mechanisms that might explain the increased fragility
-Ex: Haversion and Volkman canals offer no resistance to crack growth
-Ex: Cement lines are weak interfaces between areas with different degrees of mineralization

## Slide 6: Advanced Light Source – Berkeley, CA
User facility
Electrons accelerated to 99.9999996% speed of light
Electromagnets force electrons into circular path
Advantages:
  Better contrast
  Resolution
  Composition analysis

## Slide 7: Sample prep
Surgical removal (fresh frozen)
Machining into beams
 | Age | Location | Drug History
OI (N=10) | 10.4 | Mid-diaphysis | Bisphosphonates
Type I (n=3) |  | Femur (n=4) | Pamidronate (n=6)
Type III (n=5) |  | Tibia (n=5) | Alendronate (n=1)
Type IV (n=2) |  | Humerus (n=1) | None (n=3)
Control (N=8) | 4.5 | Diaphysis | None
Healthy Pediatric |  | Femur | 
OI: ~1 x 0.6 x 5mm
Control: ~1 x 0.2 x 10mm

## Slide 8: Healthy Pediatric vs. OI
Healthy Pediatric
Type I - Mild
Type III - Severe
Type IV - Moderate
 | Healthy Pediatric | OI | Significance?
Ca.V/TV (%) | 3.4 | 20.5 | P < 0.05
Ca.S/TV (mm-1) | 3.1 | 6.0 | n.s.
Ca.Dm (mm) | 0.041 | 0.128 | P < 0.001
Ca.Sp (mm) | 0.177 | 0.237 | n.s.
Ca.ConnD (mm-3) | 8.5 | 73 | P < 0.05
Increasing porosity (Ca.V/TV), canal diameter (Ca.Dm)

## Slide 9: Take Home Messages
Pore structure varies significantly between healthy/OI, and possibly with OI severity
Reduction in OI bone strength can (at least partially) be explained by a dramatic increase in cortical porosity and canal diameter
  Strong correlation between porosity and flexural strength (R2=0.79)
  No apparent correlation between vBMD and flexural strength

## Slide 10: Future work: Quantifying crack resistance
Fracture mechanics: Study of crack initiation and propagation (growth)
Kc – Critical “stress intensity factor”
  Ability to dissipate E before catastrophic failure (fracture)
  Increase toughness by disrupting straight crack path
    Ex: Crack deflection/twisting at central & Volkmann’s canals
Volkmann’s canal
Central canal
Crack
Canals
Koester et al 2008
Notes: -Has the potential to improve subject-specific FE models to assess fracture risk
-Finite element solvers like Abaqus are beginning to incorporate fracture toughness into models

## Slide 11: Other future applications
Effect of bone augmenting drugs
  Mineralization “mapping”
Look at degree of anisotropy
Ultrastructural studies
  SAXS/WAXD to look at collagen orientation and mineral spacing
First-order collagen peak

## Slide 12: References
Matsumoto T, Yoshino M, Asano T, Uesugi K, Todoh M, Tanaka M (2006). Monochromatic synchrotron radiation uCT reveals disuse-mediated canal network rarefaction in cortical bone of growing rat tibiae. J Appl Physiol 100: p274-280.
Matsumoto T, Yoshino M, Uesugi K, Tanaka M (2007). Biphasic change and disuse-mediated regression of canal network structure in cortical bone of growing rats, Bone 41: p239-246.
Chen H, Zhou X, Shoumura S, Emura S, Bunai Y (2010). Age- and gender-dependent changes in three-dimensional microstructure of cortical and trabecular bone at the femoral neck. Osteoporos Int 21: p627-636.
Barth RW, Williams JL, Kaplan FS (1992). Osteon morphometry in females with femoral neck fractures. Clin Orthop 283: p178-186.
Snyder SM & Schneider E (1991). Estimation of Mechanical Properties of Cortical Bone by Computed Tomography. J Orthop Res 9: p422-431.
Albert C, Jameson J, Toth JM, Smith P, Harris G (in press). Bone Properties by nanoindentation in mild and severe osteogenesis imperfecta. Clinical Biomechanics. http://dx.doi.org/10.1016/j.clinbiomech.2012.10.003
Rauch F, Travers R, Parfitt AM, Glorieux FH (2000). Static and Dynamic Bone Histomorphometry in Children With Osteogenesis Imperfecta. Bone 26: p581-589.
Boyde A, Travers R, Glorieux FH, Jones SJ (1999). The Mineralization Density of Iliac Crest Bone from Children with Osteogenesis Imperfecta. Calcif Tissue Int 64: p185-190.
Koester KJ, Ager III JW, Ritchie RO (2008). The true toughness of human cortical bone measured with realistically short cracks. Nature Materials 7: p672-677.

## Slide 13: Acknowledgements
Department of Education NIDRR grants H133P080005 and H133E100007
Marquette:
  Carolyne Albert, PhD
  Robert Molthen, PhD
  Gerald Harris, PE, PhD
Shriners:
  Peter Smith, MD
  Kathy Reiners, Motion Analysis Lab Coordinator
Berkeley:
  Dula Parkinson, PhD
  Alastair MacDowell, PhD
  Rob Ritchie, PhD
  Liz Zimmerman, PhD
http://www.tech4pod.org/